Natural Rubber R55 Test Report

| Test Item | Standard | Test Result | Conclusion |
| --- | --- | --- | --- |
| Hardness (Shore A) | 52±3 | 51 | Qualified |
| 300% Stretching Strength (MPa) | ≥4 | 4.6 | Qualified |
| Tensile Strength (MPa) | ≥21 | 24 | Qualified |
| Elongation at Break (%) | ≥500 | 590 | Qualified |
| Tensile Set at Break (%) | ≤25 | 24 | Qualified |
| Rubber to Metal Bonding Pull Strength (MPa) | ≥5 | 6 | Qualified |
| Akron Abrasion cm3/1.61km | ≤0．08 | 0．074 | Qualified |
| Acid & Alkali Resistant PH Value (Liquid) | 3-12≤65℃ | － | Qualified |
| Apprearance | Neat | Qualified |
| － | － | － | － |
| － | － | － | － |

Shijiazhuang Minerals Equipment Co., Ltd

QC Department

Oct-12th-2015